# Sub-Module 3.2: Adhesive System Types

Module 3: Dental Materials & Material Science | Sub-Module 3.2

## Note on Sources

Sources used in this document: [1] Philips' Science of Dental Materials (13th ed.) — real pH-based mild/strong self-etch mechanism, the concrete clinical-application matching guide, and 3-year randomized-trial evidence; [2] Craig's Restorative Dental Materials (14th ed.) — the specific chemistry of how mild self-etch systems bond chemically to residual hydroxyapatite, and self-etch's structural elimination of two specific etch-and-rinse failure modes. [3] McCabe JF, Walls AWG. Applied Dental Materials (9th ed.) — a specific self-etch mechanical advantage (no open-dentinal-tubule stage) and an honest critique of combining self-etch primers with a separate phosphoric-acid enamel etch, neither previously covered. [4] van Noort R, Barbour M. Introduction to Dental Materials (4th ed.) — a precise terminology distinction between "one-bottle" bonding systems and true self-etching primers, easily confused but mechanistically different. [5] Alani A, Patel M. Adhesive Techniques in Restorative Dentistry (BDJ Clinician's Guides). A genuinely modern (2020s) clinical source that fills a real gap the older textbooks in this sub-module could not: an explicit "eighth-generation = universal" framework with exact, real timing for every generation and every etch mode.

Revision note: the user asked whether McCabe's — on the standing Module 3 secondary source list — had been checked for this sub-module; it had not been. It adds a specific self-etch advantage (no stage with open, unprotected dentinal tubules) not framed this way elsewhere, plus an honestly skeptical critique of the common practice of adding a separate phosphoric-acid step to an otherwise self-etch protocol. Added below.

Second revision note: the user supplied a genuinely modern textbook, Adhesive Techniques in Restorative Dentistry (Alani & Patel, BDJ Clinician's Guides). Every other source in this sub-module predates ~2015 and does not use "universal adhesive" terminology at all — this source does, framing it explicitly as the EIGHTH generation, and gives real, exact-timing protocol tables for every generation (4th, 5th, 6th/7th, 8th) across every etch mode. This fills a genuine gap flagged earlier in this document's own notes. Added below, replacing the placeholder cross-reference in Section 3.2.3.

Revision note: continuing the audit of the newly-supplied textbooks against sub-modules given only a light check earlier. Van Noort's draws a precise, easily-confused terminology distinction between "one-bottle" bonding systems and true self-etching primers — both are two-step, single-bottle-per-step products, but they differ in whether a SEPARATE acid-etch step is still used. Added below.

Cross-reference note: Module 1's Sub-Module 3.2 already covers the general etch-strategy classification (Section 3), primer/bonding-agent chemistry, universal adhesive requirements and pH range, and a critique of "generation" numbering — that content is cross-referenced rather than rebuilt. This sub-module adds what was not previously covered: the real pH values and distinct chemical bonding MECHANISMS separating mild from strong self-etch systems (not just the label), the 2-step-vs-3-step etch-and-rinse distinction and its specific durability failure mode, a concrete restoration-type-to-system matching guide, and real 3-year clinical trial evidence comparing one-step self-etch against etch-and-rinse.

# 3.2.1 Etch-and-Rinse Systems (Total-Etch)

Full general treatment — phosphoric acid concentration/time, enamel/dentin etch mechanism, hybrid layer formation — is covered in Module 1's Sub-Module 3.2. What follows is the specific structural distinction between step counts within etch-and-rinse systems, which is genuinely new.

Two-step vs. three-step etch-and-rinse — a real durability difference, not just a convenience difference: in a two-step system, hydrophilic and ionic monomers are combined together into a single bottle applied after etching. This has a specific structural consequence: the bonded interface does NOT develop a separate hydrophobic resin layer on top, which leaves the bond susceptible to ongoing water penetration and subsequent degradation — genuinely reducing long-term bond durability compared with a three-step system, which keeps the hydrophilic primer and the hydrophobic bonding resin as separate, sequential applications specifically to build that protective hydrophobic outer layer. [1, p.268]

This is a direct, mechanistic explanation for why three-step ("fourth-generation") etch-and-rinse systems remain the recommended choice specifically for bonding composite CORES (Section 3.2.4 below) — a high-stress, long-service-life application where that extra hydrophobic barrier layer's durability benefit matters most, even though it costs an extra clinical step. [1, p.268]

## "One-Bottle" Systems vs. True Self-Etching Primers — A Precise Terminology Distinction (van Noort's)

Reducing a three-stage system (conditioner, primer, sealer) down to two components can be done in two genuinely different ways, and the resulting products are easily confused despite behaving quite differently: [4, p.116]

| System type | What's actually combined |
| --- | --- |
| "One-bottle" bonding systems | The PRIMER and SEALER (adhesive resin) are combined into one bottle — but a SEPARATE acid-etch step is still performed beforehand, exactly as in a conventional etch-and-rinse protocol. This is structurally a reduced-step ETCH-AND-RINSE system, not a self-etch system, despite the single-bottle convenience. |
| Self-etching primers | The CONDITIONER (acid) and PRIMER are combined into one bottle instead — this is the genuine self-etch mechanism, where demineralization and infiltration happen together with no separate etch/rinse step at all. |

Why this distinction matters practically: "one-bottle" bonding systems continue to rely on a separate acid-etch step before the combined primer/sealer is applied — the goal is for hybridization of the demineralized dentin and sealing of the dentinal tubules to occur SIMULTANEOUSLY during that one application. To actually achieve this in practice, many one-bottle systems require MULTIPLE applications of the primer/adhesive, not a single pass — a real technique detail easy to miss if "one bottle" is assumed to mean "one application." True self-etching primers, by contrast, genuinely eliminate the separate etch/rinse step altogether, and specifically avoid the ambiguous, technique-sensitive dentin-drying judgment call that etch-and-rinse systems require. [4, p.116]

# 3.2.2 Self-Etch Systems

Self-etch systems use an acidic monomer that conditions and primes the tooth simultaneously, without a separate rinse step. There are two genuinely distinct varieties — mild and strong — distinguished by real, different pH values AND by different underlying bonding chemistry, not merely by a marketing label. [1, p.268]

## Strong Self-Etch — Mechanism Resembles Etch-and-Rinse

Strong self-etch adhesives have a low pH (<1) — genuinely comparable to phosphoric acid's own acidity — and their documented bonding mechanism closely resembles that of etch-and-rinse systems: substantial demineralization, followed by resin infiltration and micromechanical interlock. [1, p.268]

The counter-intuitive weakness: high acidity does not translate to high bond strength here. Bond strength for strong self-etch systems — particularly all-in-one (one-step) formulations — is relatively LOW, probably because of their combination of high initial acidity AND high water content acting together against the bond. A further specific weakness of all-in-one systems: their high water content causes the cured polymer to behave as a semipermeable membrane, which increases long-term degradation by hydrolysis — the resin never fully achieves the protective hydrophobic barrier that a separate bonding-resin step would provide. [2, p.280]

## Mild Self-Etch — A Genuinely Different Chemical Bonding Mechanism

Mild self-etch adhesives have a pH around 2 — meaningfully less acidic than strong self-etch — and only partially dissolve the dentin surface, demineralizing just a few micrometers deep. Critically, this leaves a substantial amount of hydroxyapatite mineral still present WITHIN the hybrid layer, attached to the collagen fibrils rather than fully dissolved away. [1, p.268]

This residual mineral enables a real chemical bond, not just a mechanical one: specific functional monomers — 4-META (4-methacryloxyethyl trimellitic anhydride) and 10-MDP (10-methacryloyloxydecyl dihydrogen phosphate) — carry carboxyl or phosphate groups that chemically interact with this residual hydroxyapatite directly. This is a genuinely different bonding mechanism from etch-and-rinse or strong self-etch, both of which rely almost entirely on micromechanical interlock into collagen with only very weak chemical-adhesive contribution. Because of this added chemical bonding contribution, mild self-etch systems can achieve a BETTER bond to dentin than etch-and-rinse adhesives achieve. [1, p.268]

The trade-off — that same chemistry has a durability cost: because the resulting interfacial zone retains mineral content and more hydrophilic character than a fully-demineralized-and-hybridized layer, it is genuinely MORE prone to hydrolytic degradation over time. The presence of residual hydroxyapatite does offer a partial compensation, though: it may help physically protect the collagen fibrils against degradation, which is thought to be why mild self-etch systems' dentin bond durability still tests as adequate overall despite this structural vulnerability. [2, p.280]

A specific clinical weak point worth naming: sclerotic dentin. Mild self-etch systems may show relatively low bond strength specifically when applied to sclerotic dentin — a substrate already flagged elsewhere in this library (Module 1's caries/diagnosis sub-modules) as etch-resistant due to its mineral-occluded tubules. The same mineral occlusion that makes sclerotic dentin harder to etch with phosphoric acid also blunts mild self-etch's already-gentler demineralization even further. [2, p.280]

## Self-Etch's Two Structural Advantages Over Etch-and-Rinse

Beyond individual bond-strength numbers, self-etch systems as a category eliminate two specific FAILURE MODES that etch-and-rinse systems are inherently exposed to: [2, p.279]

The risk of incomplete primer/adhesive penetration into the collagen scaffold that phosphoric-acid etching has already demineralized and exposed — in etch-and-rinse, if the primer fails to fully infiltrate the depth the acid demineralized, a weak, unprotected collagen zone is left behind. Self-etch avoids this because demineralization and infiltration happen together, at the same depth, by the same acidic monomer.

The subjectivity of judging "ideal" moisture on the dentin surface before primer application — the wet-bonding technique sensitivity covered in Module 1's Sub-Module 3.2. Self-etch systems dissolve the smear layer and incorporate it directly into the hybrid layer, rather than requiring the clinician to first rinse it away and then judge a subjective moisture window before the next step.

## A Third Self-Etch Advantage, and an Honest Critique of "Enhanced" Self-Etch Protocols (McCabe's)

Beyond the two structural advantages above (Craig's), McCabe's names a third, specifically mechanical one: with the self-etch method, there is no stage in the procedure where open dentinal tubules are actually exposed, and correspondingly no risk of over-drying following a rinse step — because there IS no rinse step to over-dry after. The etch-and-rinse technique, by contrast, necessarily passes through a window where the smear layer has been dissolved and rinsed away, briefly leaving tubules open and the surface vulnerable to exactly the over-drying failure mode already covered in Module 1's Sub-Module 3.2. [3, p.208]

The honest trade-off McCabe's names directly: self-etching primer systems may not etch ENAMEL as effectively as phosphoric acid does. Some manufacturers respond to this by supplying a separate phosphoric acid solution specifically for enamel etching alongside their self-etch primer system for dentin. McCabe's is candid that this hybrid approach "rather defeats the object" — if a separate acid-etch step for enamel is needed anyway, much of self-etch's core appeal (fewer steps, no separate etch/rinse stage) is undermined. [3, p.208]

Reconciling this with the selective-enamel-etch recommendation already established: this is not actually a contradiction of the "selective enamel etch" best practice covered elsewhere in this sub-module (Section 3.2.4) — it is the same underlying tension stated more bluntly. Selective etching genuinely does improve enamel bond quality over self-etch primer alone, but McCabe's point is worth keeping precisely because it names the real cost of that improvement: added complexity that partially erodes self-etch's simplicity advantage, rather than treating selective etching as a free upgrade with no trade-off at all.

## The Generation-by-Generation Framework, With Exact Timing (Alani & Patel)

A clean, modern synthesis explicitly maps bonding-agent generation to etch strategy and bottle count — and, critically, names the EIGHTH generation as UNIVERSAL, the direct answer to "which generation is a universal adhesive?" that the older sources in this sub-module could not give: [5, p.42]

| Generation | Etch technique(s) | Primer | Adhesive |
| --- | --- | --- | --- |
| Fourth | Total-etch only (enamel 30s, dentin 15s, 37% phosphoric acid) | Separate bottle 1 | Separate bottle 2 |
| Fifth | Total-etch only (enamel 30s, dentin 15s) | Combined with adhesive | Combined with primer (one bottle) |
| Sixth | Self-etch (no separate etch step) OR selective-etch (enamel 30s only) | Separate bottle 1 | Separate bottle 2 |
| Seventh | Self-etch OR selective-etch | Combined with adhesive | Combined with primer (one bottle) |
| Eighth — UNIVERSAL | Self-etch, selective-etch, OR full total-etch — clinician's choice, same bottle | Combined with adhesive | Combined with primer (one bottle) |

The defining feature of the eighth (universal) generation, made explicit by this table: it is the ONLY generation where the same single-bottle product genuinely supports all three etch strategies — self-etch, selective-etch, AND total-etch — at the clinician's discretion, case by case. Generations four through seven are each locked to one etch philosophy (total-etch for 4th/5th, self-etch-or-selective for 6th/7th); only the 8th/universal generation removes that constraint entirely. [5, p.42]

Real, exact clinical timing — worth having precisely rather than approximately: across every generation and mode, the reported protocol uses the same core numbers consistently: 37% phosphoric acid etch at 30 seconds for enamel and 15 seconds for dentin (with an explicit "do not desiccate" caution specifically for dentin after rinsing); a primer or bonding-agent "scrub" application of 15-20 seconds; and light polymerization of 20 seconds. For the universal (8th-generation) adhesive specifically, all three etch modes converge on the SAME 20-second bonding-agent scrub and 20-second light-cure — the etch mode changes only what happens BEFORE the bonding agent is applied, not the bonding-agent application itself. [5, p.43]

# 3.2.3 Universal Adhesives — Cross-Reference Plus New Evidence

Universal adhesives' compositional requirements and the 2.2-3.2 pH performance range are already covered in Module 1's Sub-Module 3.2 (Section 3.1). What follows is real outcome evidence not previously included.

A specific 3-year randomized clinical trial finding: van Landuyt and colleagues (2011) found that a one-step self-etch adhesive showed SIMILAR overall clinical performance after 3 years compared with an etch-and-rinse adhesive, in Class V restorations specifically. However, the one-step self-etch group showed MORE incisal marginal defects and discoloration than the etch-and-rinse group over that same period — meaning "similar overall performance" is not the same claim as "equivalent on every specific failure metric," and the marginal/esthetic failure mode specifically favored the older, more established etch-and-rinse technique even in this relatively favorable trial for the newer system. [1, p.268]

A broader, honest evidence caveat: at the time Philips' was written, one-step self-etch products had undergone comparatively limited clinical study, and consequently less was known about their long-term performance and bond durability relative to the more established two-step self-etch and etch-and-rinse categories — worth keeping in mind as a general pattern (newer, more convenient systems accumulate long-term outcome data more slowly than the protocols they're replacing) rather than assuming newest is automatically best-proven. [1, p.268]

# 3.2.4 A Concrete Restoration-Type-to-System Matching Guide

Beyond the general etch-strategy classification, Philips' gives specific, restoration-type-matched recommendations — a genuinely practical synthesis worth having as a single reference table: [1, p.268]

| Clinical situation | Recommended adhesive category |
| --- | --- |
| Bonding composite CORE build-ups | Three-step, etch-and-rinse ("fourth-generation") — the extra hydrophobic-layer durability benefit (Section 3.2.1 above) matters most for a long-service, high-stress foundation restoration. |
| Bonding anterior and posterior composites; cementing veneers with resin cement | Two-step etch-and-rinse ("fifth-generation") — the best-performing option for these applications specifically. |
| Bonding posterior composites | Two-step self-etch ("sixth-generation") is the better choice here — a different recommendation from the anterior/veneer case above, reflecting posterior teeth's different isolation/access/stress profile. |
| Esthetic posts and ceramic restorations bonded with resin cement | Dual-cure, one-step self-etch ("seventh-generation") — dual-cure chemistry is specifically needed here because light may not fully reach a post space or beneath an opaque/thick ceramic restoration. |
| Bonding posterior composite restorations (light-cured route) | Light-cured, one-step self-etch ("seventh-generation") — a distinct recommendation from the dual-cure entry above, for situations where the light CAN fully reach the restoration. |

The pattern worth internalizing, not just the individual rows: there is no single "best" adhesive system across all of dentistry — the correct choice tracks the specific clinical demand of the restoration (core-build-up durability vs. posterior access vs. light-reach for a post/ceramic case), which is exactly why this module builds toward Sub-Module 6 (Material Selection & Clinical Decision-Making) rather than presenting adhesive-system choice as a solved, one-size-fits-all question.

# References

1. Anusavice KJ, Shen C, Rawls HR, eds. Philips' Science of Dental Materials. 13th ed. St. Louis: Elsevier; 2013.

2. Sakaguchi RL, Ferracane JL, Powers JM. Craig's Restorative Dental Materials. 14th ed. St. Louis: Elsevier; 2019.

3. McCabe JF, Walls AWG. Applied Dental Materials. 9th ed. Oxford: Blackwell Publishing; 2008.

4. van Noort R, Barbour M. Introduction to Dental Materials. 4th ed. Edinburgh: Mosby Elsevier; 2013.

5. Alani A, Patel M. Adhesive Techniques in Restorative Dentistry. Cham: Springer (BDJ Clinician's Guides).